## Slide 1
Astronomy Instrumentation Group - Cardiff University
RadioNet ERATec Florence, October 5th, 2015
Giampaolo Pisano
Waveguide and Metamaterial-based Quasi-Optical components for Millimetre ans Sub-millimetre Astronomy Applications

## Slide 2
Summary
Waveguide components
Metamaterial QO components
New QO developments
Introduction

## Slide 3
Cardiff AIG Group involvement: From Radio to THz
Sub-mm
Millimetre
Radio
~200mm
~1.5THz
1mm
300GHz
~100GHz
~3mm
~300MHz
~1m
BINGO
Quijote
2025?
2015
FAST
SRT
Balloon borne
Satellite
QUBIC
COrE+ / LiteBird
60 – 600 GHz / 60 – 280 GHz
~1 GHz
10 - 40 GHz
150 GHz
(90-220)
0.6 - 1.6 THz
~1 GHz
ArTemis
0.3 - 115 GHz
LSPE
90 – 220 GHz
Ground based
Pilot/Blast TNG
0.5 – 1.2 THz /0.5 – 1.4 THz
100 - 300 GHz
NIKA2
Notes: etendue domaine de frequence
Strategie: collecter des donnes, developpment instrument et planification d’instruments futurs
Livraison de donnees domaine astro large (JBCA Pulsars, Cosmologie, CMB, star formation)
Differents types de contribution  intro de Planck et futurs projets

## Slide 4
LSPE - SWIPE instrument
P. de Bernardis et al.,
Proc. SPIE v.8452 (2012)
140, 220 & 240 GHz
Thermal Filters
Wire-grid Polariser
Rotating HWP
Band defining
Filters
Thermal Filters
Astronomical instrumentation: CMB instrument example
 All the QO components can be realised using the Mesh Technology
Cryostat window ARC
Dielectric Lens
300K
130K
30K
2K
300mK
Stage temperatures
Waveguide
components
Horns, OMTs,...

## Slide 5
RF components development for Astronomical Instrumentation
Corrugated
horns
Ortho-Mode Transducer (OMT)
Mandrel
B.Maffei
Aluminium
Mandrel
W-band
W-band
Equi-Phase
OMT
Filter
90° Microstrip
Hybrid
Phase
Shifters
W-band
W-band
W-band
W-band
Polarisation Modulator
Circular Polariser
Polarimeters Array
W-band
W-band
Q-band

## Slide 6
OMT v.1
OMT v.2
OMT v.3
Cross-pol ~ -42/-50dB
Pisano et al. - IEEE MWCL (2007)
Return Loss ~ -26/-28 dB
Insertion Loss ~-0.2/-0.3 dB
W-Band Ortho-Mode Transducer

## Slide 7
Pisano et al. – IEEE MWCL (2011)
- Waveguide transposition of a Pancharatnam recipe used in optics
DF < 1 deg
X-pol ~ -37dB
W-Band Polarisation Rotator

## Slide 8
DF < 1 deg
AU ~ 0.04 dB
- Waveguide transposition of a Pancharatnam recipe used in optics
Pisano et al. – JEMWA, v.26,
n.5/6, pp 707-715 (2012)
Q-Band Circular Polariser
FP7 - Apricot Project

## Slide 9
INAF Medicina, INAF Arcetri, Cardiff University
Platelet
Corrugated
Horn
Polariser
Platelet
OMT
LNAs
Freq. range: 0.3 – 115 GHz
Diameter: 64m
19-beams Q-band receiver array
Application of the Q-band polariser: Sardinia Radio Telescope
A. Orfei
R. Nesti
P. Bolli
G. Pisano

## Slide 10
Mesh Wave Plates
Mesh Lenses
Photolithographic Mesh-Filters
Dielectrically Embedded Filters
Dichroics
NRI Lenses & Wave Plates
OAM Q-plates
Mesh Lens arrays
Quasi-Optical components & Metamaterials development

## Slide 11
Inductive High-Pass Filter
Resonant Band-Pass Filter
Mesh Technology: Modelling
Capacitive Low-Pass Filter
Grid Period
Equivalent Circuit
Spectral response
< l
Sub-wavelength periodic structures
Markuvitz (1951)
Ulrich (1967)
FSSs subgroup

## Slide 12
The manufacturing process
Copper evaporation on polymer substrate
Photolithographic etching to form metal grid pattern
Randomly oriented grids precisely spaced and mounted together to form a single composite filter.
Air/vacuum gap filters use annular metal spacers
Mesh Technology: Manufacture 1/2
Press tools
Metal grids
Spacers
Filter support
rings
Free standing (air-gap) multiple metal mesh devices
=50cm
 Large diameters achievable: 0.5m 
Carole Tucker and Peter Ade

## Slide 13
Dielectrically embedded multiple metal mesh devices
The manufacturing process
Grids production and arrangement as for air-gap filters
Polypropylene layers used as dielectric spacers
Hot pressing process to bond the whole structure together into a single device
They are robust, can be cryogenically cooled, space qualified
They can be cut to any shape
Ex: 100GHz low-pass filter
Mesh Technology: Manufacture 2/2

## Slide 14
Mesh Filters: Band defining example
FSSs
Homogeneous
grids
Chart: wavenumber (cm-1)
Low Pass Capacitive Hot Pressed Mesh Filters (10 grids )
P.Ade, C.Tucker
- Hot pressed high frequency rejection continues through diffraction region
Chart: Wavenumber [cm-1]


## Slide 15
- Essential components for multi-frequency photometers
- Allow simultaneous imaging of the source in several wavebands
- Wood’s anomalies increase with off-axis incidence angle and beam convergence
Dichroics: Frequency Splitters
Chart: Wavenumber [cm-1]
Capacitive grid air-gap with f/4 beam at 30deg incidence angle
P.Ade, C.Tucker

## Slide 16
G. Pisano et al.
Appl.Opt. v47, n33 (2008)
Capacitive Stack
Inductive Stack
- Rotating HWPs are used to rotate/modulate linear polarisation
Dj = p
Shatrow geometry
Homogeneous
anisotropic
grids
Mesh Half Wave Plates: First air-gap design

## Slide 17
Mesh Half Wave Plates: Embedded design
Homogeneous
anisotropic
grids
Lerner geometry
Other devices:
QWPs (linear circular)
=20cm
W-Band
G. Pisano et al.
PIER M, 25, p101 (2012)
Unit cell

## Slide 18
Transmission along C-axis
Transmission along L-axis
45 Cross-Polarisation
~90% BW
Mesh HWPs: Large bandwidth designs BW~90%

## Slide 19
ESA-TRP
collaboration
Cardiff Manchester
Rome
RAL
0
p
ER-HWP
x
y
Embedded Reflective HWP: Very large bandwidth BW~150%
Cross-polarisation
Modulation efficiency
~150% BW
- Metamaterial based reflecting devices working up to 45 deg incidence angles

## Slide 20
Flat Mesh Lens: Inhomogeneous Phase Delays
Locally variable
grid geometries
Multiple transmission lines
- Very thin and robust
- Very light and low loss
- No Anti Reflection Coatings required
Inhomogeneous
grids
W-Band f/3 lens prototype (1.4mm thick)
54 mm Ø
G. Pisano et al.
Applied Optics 52,n.11, (2013)

## Slide 21
Flat Mesh Lens: Transmission line design
G. Pisano et al.
Applied Optics 52,n.11, (2013)
- Lens consisting of ~ 8000 TLs
- Solution of just 1/8 of the surface
- Optimisation for max transmission &
appropriate differential phase shift
Flat lens made with 10 grids (5+5)

## Slide 22
2D model (cylindrical)
Central TL array
3D full model
Flat Mesh Lens: Finite-element modelling
G. Pisano et al.
Applied Optics 52,n.11, (2013)

## Slide 23
 Experimental agreement down to the 4th side lobes
Flat Mesh Lens: VNA beam tests
G. Pisano et al.
Applied Optics 52,n.11, (2013)

## Slide 24
Flat Mesh Lens Array: Focal plane detector/antenna integration
- Mesh lens miniaturisation for large focal plane arrays
- Usual manufacturing processes, accurate alignment required
- A single flat device includes all the lenses
ESA TRP collaboration: Maynooth (PI), Manchester, Cardiff, Rome, Paris APC and Chalmers
10 mm
W-band

## Slide 25
Mesh-based QO devices
- Low pass & high pass
- Band pass
- Blocking filters
- Neutral density
Filters
- We have discussed only a few devices developed using the mesh technology
- Artificial dielectrics
- Artificial birefringent materials
- Anti-Reflection Coatings (ARCs)
- Negative Index metamaterials
- Artificial Magnetic Conductors
- Mesh Absorbers
Metamaterials
- Mesh HWP
- Mesh QWP (circ.polariser)
- Reflective HWP
- Spiral Phase Plate
Retarders
- Graded index lens
- Mesh lens
- Mesh lens array
- Negative index lens
Flat lenses
- Many of these are standard solutions adopted in mm-wave and THz
astronomical instrumentation
- Some of the most recent solutions are currently finding their applications
- More ‘exotic’ devices are currently under development..
- Beam divider
- Dichroic
- Polariser
- Polarisation splitter
- Mesh Prism
Dividers

## Slide 26
Mesh Trichroic for triple-feed simultaneity: Conceptual idea
x=0
x=d
n3
n2
n1
DJ
Same mesh recipe
for fixed x
- It’s not a focusing component
- It’s re-directing radiation in different directions depending on frequency
- Same direction within same bands
 Design of highly transmissive ‘mesh-filters lines’ with complex phase behaviour
Dn1
Dn2
Dn3
DJ
n
n1
n2
n3
a
-a
- Can we design a mesh-device able to redirect beams at different frequencies?
See A.Orfei Talk:
“Multi-frequency observations
using multifeed systems”

## Slide 27
Mesh Trichroic for triple-feed simultaneity: Conceptual idea
- The frequency-dependent differential phase-shift, respect to a fixed point
(ex: centre), would create the required off-axis phase-fronts at the output
- Real converging beams will require additional optimisation
 This is an ongoing development
n1 ± Dn1
n2 ± Dn2
n3 ± Dn3

## Slide 28
Conclusions
Waveguide development:
  Alternative designs based on recipes used in optics
Metamaterial mesh-devices development:
  Very broad range of components available
  Very accurate modelling, manufacture and testing now achievable
New exotic mesh-devices:
  Local, frequency dependent arbitrary manipulation of :
    Transmitted/reflected amplitudes
    Transmitted/reflected phases
    Polarisation states
    ‘Equivalent’ refractive index and dispersion
    ‘Equivalent’ birefringence

## Slide 29
The End
Thank you!